## Slide 1: Lithography & Patterning
Evan Chen

## Slide 2: Overview
Review of Fabrication Techniques
Lithography Over the years
Lithography Types & Settings
Physics Behind Lithography
Future State of Lithography

## Slide 3: What is Lithography? Why is Lithography? (How is Lithography?)
Let’s say you wanted to build a full adder out of transistors

## Slide 4: What is Lithography? Why is Lithography? (How is Lithography?)

## Slide 5: What is Lithography? Why is Lithography? (How is Lithography?)

## Slide 6: What is Lithography? Why is Lithography? (How is Lithography?)

## Slide 7: What is Lithography? Why is Lithography? (How is Lithography?)

## Slide 8: What is Lithography? Why is Lithography? (How is Lithography?)

## Slide 9: What is Lithography? Why is Lithography? (How is Lithography?)

## Slide 10: What is Lithography? Why is Lithography? (How is Lithography?)
60µm = 60,000nm
14nm

## Slide 11: What is Lithography? Why is Lithography? (How is Lithography?)

## Slide 12: What is Lithography? Why is Lithography? (How is Lithography?)
Human hair diameter (60µm)
14nm FinFET

## Slide 13: What is Lithography? Why is Lithography? (How is Lithography?)
Probably not going to be able to wire 14nm transistors using hands, tools, machines, etc…

## Slide 14: What is Lithography? Why is Lithography? (How is Lithography?)
The solution?
LITHOGRAPHY!
Basically, we’ll design our transistors and circuits using light
What is Lithography?
Method of transferring circuit design to silicon wafer
  Patterns are too small to be transferred physically
  Light has wavelength in scale ~nm
  Followed by less precise “blanket techniques”

## Slide 15: Fabrication Techniques
Lithography (Framing)
Implantation (Modification)
Deposition (Additive)
  Oxidation
  Plating
Etching (Subtractive)
  Wet, Dry

## Slide 16: Fabrication Techniques - Lithography
Technique used to define where you want a pattern to be
Involves wavelengths of light reacting with a chemical (photoresist)
Material can be added/removed between the photoresist

## Slide 17: Fabrication Techniques - Implantation
Used to modify properties of the wafer underneath
In Silicon, dopants may result in excess electrons or holes (N, P-type)
Slight changes in concentration results in large change in electrical conductivity (~100x)
Always causes damage to substrate- must be repaired with an anneal step

## Slide 18: Fabrication Techniques - Deposition
Additive technique for wafer fabrication
3 (main) types
  Oxidation
  Deposition
    Many sub-categories:
      CVD, LPCVD, PVD, PECVD…
  Electroplating

## Slide 19: Fabrication Techniques - Etching
Two important characteristics
Selectivity: How quickly one material is etched relative to another
Anisotropy Ratio: How quickly material is consumed in a certain direction versus another
Two main types
Wet Etching (Typically with acids/other wet chemistry)
Dry Etching (Typ. Reactive Ion Etching)

## Slide 20: Lithography Over the Years
What is the goal when optimizing the lithography process?
  Better resolution!

## Slide 21: Lithography Over the Years
What is the goal when optimizing the lithography process?
  Better resolution!

## Slide 22: Lithography Over the Years- Characteristic Equation
CD: Critical Dimension (Minimum feature size)
K1: Process Coefficient
  Typ. 1, Can go to ~0.5 or lower
Lambda: Wavelength of incoming light
NA: Numerical Aperture
  Typ. 0.5-0.7, can go above 1
We’ll come back to this…

## Slide 23: Lithography Over the Years- Wavelengths
Mercury Lamp (UV)
  G-line (436nm), H-line (405nm), I-line (365nm)
Excimer Laser (DUV)
  KrF (248 nm)
  ArF (193nm)
EUV (13.5nm)

## Slide 24: Lithography Over the Years- Wavelengths
????
https://www.youtube.com/watch?v=ZPa_RKFTBPc

## Slide 25: Lithography Over the Years- Why 193???
Before 1990:
  “Like drawing thick lines with a sharp pencil”
After 1990
  “Mask Designer’s Nightmare”

## Slide 26: Lithography Over the Years- What happened to 157?
  Technical Challenges:
  Poor Photoresist
  Needed new reticle design
  Expensive processing
  Upcoming Solutions (for 1990s)
  Immersion technology!?
  EUV supposed to come out in 2001

## Slide 27: Lithography Over the Years- What happened to 157?
  Technical Challenges:
  Poor Photoresist
  Needed new reticle design
  Expensive processing
  Upcoming Solutions (for 1990s)
  Immersion technology!?
  EUV supposed to come out in 2001
    (GTA6 of Semiconductor Industry)

## Slide 28: Brute Force for Moore’s Law (k1)
Resolution Enhancement Techniques
Optical Proximity Correction
Phase Shift Masks
Double Patterning Techniques
(image unrelated)

## Slide 29: Brute Force for Moore’s Law (k1) - OPC
Optical Proximity Correction (OPC)
Constructive/Destructive Interference
  Introduce serifs/additional patterns so OUTPUT looks correct (mask doesn’t)
  VERY interesting field for optics engineering & computer science

## Slide 30: Brute Force for Moore’s Law (k1) - Phase Shift Masks
Phase Shift Masks
Control interference for better feature fidelity

## Slide 31: Brute Force for Moore’s Law (k1) - Phase Shift Masks
  Phase Shift Masks
  Mask Design No longer Binary
  Designed constructive/destructive interference for high-resolution output

## Slide 32: Brute Force for Moore’s Law (NA) - Immersion Lithography
  Immersion Lithography
  Increase Numerical Aperture (Sharper Focusing of light)

## Slide 33: Brief Aside - The issue with NA
  Depth of Focus (DoF)
  More precision in distance from lens
  In EUV, photoresist needs to be ~10s of nm thick
  DoF inversely proportional to NA

## Slide 34: Brute Force for Moore’s Law (k1) - Double Patterning
  Solve interference problem by just making more masks
    2x, 4x patterning
  POV: Mask designers selling more masks to do the same work

## Slide 35: Mask Design
Exposure Area:
Limited by Reduction Lenses
~26x33 mm max
DUV/Older systems:
Quartz (Fused Silica)
Chromium
Can cost ~10-100k
https://youtu.be/9RZreu5z_Gc?si=rI32Z36lvvmAOuUl

## Slide 36: Mask Design (EUV)
Extremely Expensive
“Mirror mask”
~70% of energy is absorbed
  11 mirrors -> 0.7^11 = 2% energy transfer
50+ layers of Molybdenum + Silicon
Can cost ~500k each

## Slide 37: Mask Design (EUV)

## Slide 38: Photoresist
  Large, Organic polymers
  When exposed to light, cross-linking occurs between polymers
  Good photoresist requires the following
    Specific wavelength sensitivity
    High uniformity
    Very strong chemical resistance (When exposed)
    Easy development (Removal of “blank” areas)
    Limiting factor for new wavelengths!

## Slide 39: Weird Photoresist (EUV)
Etch rate additives
Actual resist is too thin to work long enough…
BARC/Underlayers
Reduce “Standing waves”
Improve adhesion/resolution

## Slide 40: Lithography Types- “Choose your own adventure”
Contact
Non-Contact
Projection
E-Beam*

## Slide 41: Lithography Types- “Choose your own adventure”

## Slide 42: Lithography Types- Performance Comparison
Parameter | Contact | Non-Contact | Projection | E-beam
Cost | Low | Low | High | High
Speed | Med | High | High | Low
Defectivity | Very High | Low | Low | Low
Resolution | Med | Low | High | Very High
Complexity | Low | Med | High | Med
Each are useful!
  Which would you use for…
    Academic (Very low volume)
    Industry (High Volume)
    Research

## Slide 43: Lithography Procedure
Spincoat
Soft-Bake
Expose
Post-exposure Bake (Optional)
Develop
Hard-Bake

## Slide 44: Lithography Procedure- Spincoat

## Slide 45: Lithography Procedure- Softbake
Solidify photoresist
Removes solvent
Can be done with hotplate in research applications
Integrated in lithography machine for industry applications

## Slide 46: Lithography Procedure- Exposure
Align with previous layers of mask
Use lightsource (EUV, DUV, etc) to bond photoresist

## Slide 47: Lithography Procedure- Develop
Dissolves un-bonded photoresist

## Slide 48: Lithography Procedure- Modern Systems
https://youtu.be/h_zgURwr6nA?si=Jx0LdQDefZiJwbs1

## Slide 49: Future State of Lithography
High-NA EUV Resolution Enhancement Techniques
Higher Power Source (Free Electron Laser)
Larger exposure field? (Reticle)
Mechanical Improvements for High-Throughput/Precision
Cutting Cost???

## Slide 50: The End
Thanks for listening!